**Apparel Check List (General Use)**

**(clothing, wearables, sashes, hats, scarves, mittons)**

**Garment Requirements**

[ ]  Lead Content in Paint and Similar Surface Coatings (16 CFR 1303)

[ ]  Total Cadmium in clothing (Detachable ornaments which are similar to an anklet, arm cuff, bracelet, charm, brooch, chain, crown, cuff link, watch: <300 ppm)

[ ]  Flame Retardants: PentaBDE, OctaBDE, DecaBDE, TCEP. No detection.

[ ]  Fiber Content/Analysis AATCC 20/20A

*Testing not required if vendor provides data.*

[ ]  Flammability of wearing apparel. 16 CFR 1610

[ ]  Flammability of vinyl material. 16 CFR 1611

 *Testing not required if no vinyl present in garment.*

[ ]  Flammability of Solids. 16 CFR 1500.44

 *Testing not required unless accessories present.*

[ ]  Drawstrings (No drawstrings in the hood and neck area ; drawstrings at waist and bottom may not extend more than 3” past channel when garmet is expanded to fullest width; no toggles, knots or other atttachments at free ends; bartacked if drawstring is one continuous string (applies to products intended for individuals up to 16 years of age, including age 16)

[ ]  Care Labeling. 16 CFR 423

*Testing not required and a visual inspection is ok provided the vendor provides the information.*

[ ]  Textile Fiber Products Identification/RN#.16 CFR 303/300

 *Testing not required; visual inspection ok.*

[ ]  Country of Origin Marking. 19 CFR 134.11

 *Testing not required; visual inspection ok.*

[ ]  General Certificate of Conformity (“GCC”)

[ ]  Recent Test Report

**California Prop 65**

[ ]  Lead in Substrates and Surface Coatings <90 ppm

*May use CPSIA lead testing data. Additional testing typically not required.*

[ ]  Phthalates (DBP, BBP, DEHP, DINP, DIDP, DnHP)

*Testing may not be necessary if no plastic components. Consult with Anseco on a case by case basis.*

[ ]  Total Cadmium in Surface Coatings and Substrates

[ ]  Bisphenol A (BPA) (<100PPT)

***A warning label on the product, packaging and marketing materials will be required for products going into California if phthalates/Cadmium/BPH is in excess of the safe harbor limits. If lead is in excess of the 90/100 ppm, the product may not be sold anywhere in the United States as the product would be deemed a banned hazardous substance.***

**Packaging Requirements**

[ ]  TPCH/Coneg/Toxic Elements in Packaging Material (sum of cadmium, hexavalent chromium, lead and mercury in packaging and packaging components shall be < 100ppm by weight)

[ ]  Plastic Bag Warning. **“Warning: To avoid danger of suffocation, keep this plastic bag away from babies and children. Do not use this bag in cribs, beds, carriages or playpens. This bag is not a toy.”**

*Testing not required; visual inspection is ok.*

[ ]  Prop 65 Warning Label if phthalates, cadmium and/or BPA in excess of the safe harbor limits is present.

**Marketing Material Requirements**

[ ]  Prop 65 Warning Labels (including on websites, catalogs)

Version Control

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
| **Version** | **Description** | **Document #** | **Effective Date** | **Created by:** |
| 1 | Apparel Check List (General Use) | 902121\_1 | 07/20/2016 | Emily Rudie |
| 2 | Apparel Check List (General Use)* Clothing, wearables, sashes, hats, scarves, mittons, added to description
 | 902121\_2 | 07/21/2016 | Emily Rudie |