**Drinkware/Food Contact Check List (Children’s)**

**Product Requirements**

Lead in Paints and Surface Coatings. 16 CFR 1303, CPSIA Section 101 (<90ppm)

Test conducted by Accredited Third Party Lab.

Test conducted within the past 12 months.

If lead is >40ppm but <90ppm, IL warning required.

*Testing not required if the article contains no surface coatings/paints.*

Total Lead in Substrates. CPSIA Section 101, (<100ppm).

Test conducted by Accredited Third Party Lab.

Test conducted within the past 12 months.

If lead is >40ppm but <90ppm, IL warning required.

Bisphenol-A Content (BPA). No detectable levels.

Flammability of Solids. 16 CFR 1500.44

Hazardous Substances – Toxicological Risk Assessment. 16 CFR 1500.3/ASTM F963, Sec. 4.3.1

Formaldehyde in Children’s Products. MN Chapter 325F, Sec. 176-178

Sharp Points. 16 CFR 1500.48

Sharp Points (Metal or Glass). 16 CFR 1500.49

Small Parts. 16 CFR 1500.50/16 CFR 1501

Tracking Label. CPSIA 103;

*Testing not required. Visual inspection is ok.*

* Permanently affixed to product
* Name of Manufacturer
* Location of Manufacture
* Date of Manufacture
* Unique Tracking Number

Food Contact Plastic and Polymeric Coating 21 CFR 175, 21 CFR 176, 21 CFR 177, 21 CFR 180.22, 21 CFR 181.32

*as applicable*

Leachable Cadmium and Lead from Interior of Ceramic Article US FDA CPG 7117.06 and 7117.07

*If Ceramic and applicable*

*Cd: <0.25 ppm (pitchers)*

*<0.5 ppm (cups, mugs)*

*Pb: <1.0 ppm (large pitchers)*

*<2.0 ppm (small pitchers)*

*<0.5 ppm (cups, mugs)*

Leachable Cadmium and Lead from Rim Decorated Ceramic and Glass Drinking Articles. SGCD/ASTM C927

*Food contact ceramic and glass drinkware decorated within top 20 mm of lip and rim area shall not exceed the following*

*Cd: <0.4 ppm*

*Pb: <4.0 ppm*

Leachable Lead from Silver Plated Metalware. FDA CPG 7117.05

*Shall not exceed 7.0 ppm (adult); 0.5 ppm (children/infant)*

Stainless Steel Only: FDA GRAS Specifications, Total Chromium in Stainless Steel

Country of Origin Marking. 19 CFR 134.11

*Testing not required; visual inspection ok.*

Children’s Product Certificate

Recent Test Report (less than 12 months old)

**California Prop 65**

Lead in Substrates and Surface Coatings <90 ppm

*May use CPSIA lead testing data. Additional testing typically not required.*

Phthalates (DBP, BBP, DEHP, DINP, DIDP, DnHP)

Total Cadmium in Surface Coatings and Substrates

Bisphenol A (BPA) (<100PPT)

***A warning label on the product, packaging and marketing materials will be required for products going into California if phthalates/Cadmium/BPH is in excess of the safe harbor limits. If lead is in excess of the 90/100 ppm, the product may not be sold anywhere in the United States as the product would be deemed a banned hazardous substance.***

**Packaging Requirements**

TPCH/Coneg/Toxic Elements in Packaging Material (sum of cadmium, hexavalent chromium, lead and mercury in packaging and packaging components shall be < 100ppm by weight)

Plastic Bag Warning. **“Warning: To avoid danger of suffocation, keep this plastic bag away from babies and children. Do not use this bag in cribs, beds, carriages or playpens. This bag is not a toy.”**

*Testing not required; visual inspection is ok.*

Prop 65 Warning Label if phthalates, cadmium and/or BPA in excess of the safe harbor limits is present.

Tracking Label

IL Lead Warning

*Required if lead is between 40 ppm – 90 ppm and not on product directly*

**Marketing Material Requirements**

Warning Labels if applicable.

*Must be on all marketing materials (website, catalogs, etc.)*

Prop 65 Warning Labels (including on websites, catalogs)

Version

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
| Version | Document # | Title | Date Created | Author |
| 1 |  | Children’s Totes and Bags Check List (not including leather bags or lunch bags/food contact bags) | 05/02/2016 | ELR |